## Slide 1
Laser-Induced Hydrophobicity
on Thin Film Surfaces
A Review of Four Research Studies on Excimer & Nanosecond Laser
Surface Modification Techniques
Cp303
Palavalasa Bhargav

## Slide 2
What is Hydrophobicity? — The Lotus Effect
Contact Angle (θ)
The angle formed at the liquid–solid–vapour interface. Measured using sessile drop method.
Surface Type | Contact Angle (θ) | Wetting Behaviour
Superhydrophilic | θ < 10° | Complete wetting
Hydrophilic | 10° < θ < 90° | Partial wetting
Hydrophobic | 90° < θ < 150° | Low wettability
Superhydrophobic | θ > 150° | Lotus effect / self-cleaning
Wenzel Model: Liquid fills surface grooves → enhanced wettability. Cassie-Baxter Model: Air trapped in grooves → reduced contact area → superhydrophobicity.
Fig1: lotus effect

## Slide 3
Why Do We Need Hydrophobicity?
🦠 Anti-Bacterial Surfaces
Superhydrophobic surfaces entrap air at the liquid–solid interface, preventing direct bacterial contact. This is vital for medical implants, catheters, and surgical tools.
🔬 Anti-Fouling & Self-Cleaning
Water droplets roll off carrying contaminants. Key in marine coatings, solar panels, and optical lenses.
💧 Microfluidics & Lab-on-Chip
Precise control of droplet movement on Si wafers enables miniaturised diagnostic devices and biosensors.
⚡ Electronics & Semiconductors
Hydrophobic PVDF surfaces enable moisture-resistant piezoelectric sensors and integrated circuits.
🏥 Biomedical Implants
Controlled wettability reduces protein adsorption and platelet activation on implant surfaces, improving biocompatibility.
✈️ Aerospace & Automotive
De-icing, drag reduction, and corrosion resistance are achievable on metal surfaces via superhydrophobic coatings.
Source: Sohrabi et al. (2022); Liu et al. (2014); Dongre et al. (2023); Liu et al. (2010)

## Slide 4
Techniques to Generate Hydrophobicity
SURFACE ROUGHNESS METHODS
Laser Texturing
ns/fs pulsed lasers create micro/nano structures (ablation threshold creates surface topography)
Chemical Etching
Acid or base solutions roughen metal/polymer surfaces to increase contact angle
Ion-Beam Lithography
Focused ion beams pattern nanostructures on Si surfaces
Photolithography
UV-patterned photoresist used to create ordered micro-pillars
Solution Immersion
One-step process on copper/metal substrates for non-flaking superhydrophobic surfaces
SURFACE CHEMICAL MODIFICATION
UV Laser + Methanol (Si)
ArF excimer laser dissociates CH₃OH → –OCH₃ radicals bond to Si surface, reducing surface energy
KrF Laser on PVDF
Photochemical changes create C–CF₂ and C–F bonds, reducing surface energy
Spray Coating
Low surface energy materials (ZnO, fluoropolymers) applied as hydrophobic coating
Self-Assembled Monolayers
Organic molecules adsorb onto surfaces to form oriented hydrophobic layers
Plasma Treatment + SAMs
Plasma creates reactive sites; SAMs then lower surface energy selectively

## Slide 5
How to Measure Hydrophobicity
💧 Sessile Drop Method
A small water droplet (~3–5 µL) is placed on the surface. The profile of the drop is captured with a CCD camera. The contact angle θ is measured from the drop profile at the solid–liquid–vapour interface.
Used in: All four studies reviewed
🔭 Ramé-Hart NRL Goniometer (Model 100)
A precision optical goniometer. The sample is placed on a stage, a drop is dispensed via a microsyringe, and the angle is measured optically. Four independent measurements per site for accuracy.
Used in: Liu et al. (2014) – Si/methanol study
📐 OCA20 Contact Angle Meter (DataPhysics)
Automated video-based system. Measures static, advancing, and receding contact angles. Volume of drop is precisely controlled (3 µL).
Used in: Liu et al. (2010) – PVDF study
🔬 AFM — Atomic Force Microscopy
Measures surface roughness (R_RMS). Surface topography is mapped in tapping mode over 5×5 µm regions. Roughness determines if hydrophobicity is morphology-driven.
Used in: Liu et al. (2014); Liu et al. (2010)
🖥️ SEM — Scanning Electron Microscopy
High-resolution imaging of laser-induced micro/nano structures. Reveals surface morphology changes such as ablation craters, conical structures, and wall-like formations.
Used in: Sohrabi et al. (2022); Dongre et al. (2023); Liu et al. (2010)
⚛️ XPS — X-ray Photoelectron Spectroscopy
Identifies surface chemical bonds. Confirms formation of Si–OCH₃ (hydrophobic) or C–CF₂/C–F bonds on PVDF after laser irradiation.
Used in: Liu et al. (2014); Liu et al. (2010)

## Slide 6
EXPERIMENT 1
Hydrophobicity Generation
on Silicon (Si 001)
Excimer Laser-Assisted Chemical Process for Formation of
Hydrophobic Surface of Si (001)
— Liu, Hassen & Dubowski (2014)

## Slide 7
Exp. 1 — Si (001): Experimental Setup
Sample:
P-doped (n-type) Si (001) wafers; 12×6 mm; resistivity 3.1–4.8 Ω·m
Pre-treatment:
Cleaned with Opticlear, acetone, IPA (5 min each); HF etch (1:50, 1 min) to remove native oxides
Irradiation Medium:
Samples immersed in degassed methanol (CH₃OH) in a 0.74 mm microfluidic chamber
Laser (Primary):
ArF excimer laser — λ = 193 nm; fluences 30, 65, 80 mJ/cm²; up to 1000 pulses
Laser (Control):
KrF excimer laser — λ = 248 nm; up to 250 mJ/cm² (used for comparison)
Post-treatment:
Rinsed with DI water, dried with N₂, stored in sealed N₂ container
Key Principle:
ArF laser (193 nm) photodissociates CH₃OH → –OCH₃ radicals bind to Si dangling bonds → Si–OCH₃ (hydrophobic)
Key Chemical Mechanism
1. ArF laser (193 nm) irradiates Si immersed in methanol 2. Photodissociation: CH₃OH → H• + •OCH₃ radicals 3. –OCH₃ radicals bond to Si dangling bonds 4. Si–(OCH₃)ₓ compound forms → lowers surface energy 5. Result: CA increases from 77° → 103° 6. KrF (248 nm) CANNOT photodissociate CH₃OH → no effect

## Slide 8
Exp. 1 — Si (001): Results — Contact Angle & AFM Analysis
Fig. 2 – Contact angle vs. pulse number for ArF laser (Liu et al., 2014)
Fig. 3– AFM images: non-irradiated (left) vs. 500-pulse irradiated (right)
Key Findings — AFM & Contact Angle
• CA increased: 77° → 103° at 65 mJ/cm², 800 pulses • AFM roughness: 0.31 nm (ref) vs. 0.37 nm (irradiated) — NO morphology change • Hydrophobicity is purely chemical (Si–OCH₃), not structural • KrF laser showed NO change in CA (cannot break CH₃OH)
Saturation at 103°: Surface energy limited by CH₃ packing. Stability: CA stable for 4 h in N₂; drops to 56° after 20 h in air (SiO₂ oxidation).

## Slide 9
Exp. 1 — Si (001): XPS Characterisation
Fig. 4 – XPS Si 2p, O 1s, C 1s spectra: non-irradiated (a–c) vs. ArF laser irradiated 500 pulses at 65 mJ/cm² (d–f) (Liu et al., 2014)
Si 2p Peak
Si–(OCH₃)ₓ concentration: 0.7% (ref) → 3.5% (irradiated). 5-fold increase confirms –OCH₃ bonding.
O 1s Peak
Si–(OCH₃)ₓ peak at 532.6 eV increases from 1% → 2.5%. Confirms oxygen bonding through methoxy groups.
Conclusion
Hydrophobicity of Si is entirely due to chemical modification (Si–OCH₃), not surface roughness change.

## Slide 10
EXPERIMENT 2
Superhydrophobic-Antibacterial
Polycarbonate Fabrication
Using Excimer Laser Treatment
— Sohrabi, Pazokian, Ghafary & Mollabashi (2022)

## Slide 11
Exp. 2 — Polycarbonate: Setup & SEM Surface Morphology
Experimental Parameters
Sample:
PC (Polycarbonate) 1 mm thick, 1×1 cm, cleaned with water & alcohol
Laser:
KrF pulsed excimer — λ = 248 nm, 25 ns pulse, 2 Hz rep. rate
Fluence range:
Below, near & above ablation threshold (20–100 mJ/cm²)
Ablation threshold:
~40 mJ/cm² (single pulse for PC at 248 nm)
Pulses:
2000 pulses per sample
Wettability:
Sessile drop method; each condition repeated 5 times; ±2° error
Antibacterial:
E. coli adhesion test with gram staining (OD₆₀₀ ≈ 0.5)
Fig. 5 – SEM images at 2000 pulses: (a) 20, (b) 30, (c) 60, (d) 70, (e) 80, (f) 90 mJ/cm² (Sohrabi et al., 2022)
Below ablation threshold (<40 mJ/cm²): no microstructures. Above threshold: melting + rapid re-solidification → micro-scale structures → increased roughness → superhydrophobicity at >80 mJ/cm².

## Slide 12
Exp. 2 — Polycarbonate: Wettability & Antibacterial Results
Fig. 6 – Water contact angle vs. laser fluence (2000 pulses) (Sohrabi et al., 2022)
Fig. 7 – Gram-stained E. coli: (a) untreated PC, (b) superhydrophobic 80 mJ/cm², (c) hydrophobic 70 mJ/cm²
Wettability Results
< 38 mJ/cm²: Hydrophilic (θ ↓ to 51°). 60–70 mJ/cm²: Hydrophobic (θ ~90–120°). > 80 mJ/cm²: Superhydrophobic (θ > 150°). Carbonization + double-scale roughness + air pockets = superhydrophobicity.
Antibacterial Results
Superhydrophobic PC (>80 mJ/cm²): NO E. coli adhesion. Hydrophobic (~70 mJ/cm²): some adhesion. Pristine PC (θ ≈ 91°): highest adhesion. Air pockets block direct bacteria–surface contact.

## Slide 13
EXPERIMENT 3
Hydrophobicity of
Poly(Vinylidene Fluoride) — PVDF
Increasing the Hydrophobic Property of PVDF by KrF Excimer Laser Irradiation
— Liu, Wei, Jiang & Nie (2010)

## Slide 14
Exp. 3 — PVDF: Setup & Contact Angle Results
Experimental Parameters
Sample:
PVDF film, 0.5 mm thick, irradiated vertically in air
Laser:
Lambda Physik LPX305iF KrF — 248 nm, 30 ns, 50 Hz max, 1 Hz used
Fluence range:
100 – 400 mJ/cm² (E from 50 to 600 mJ/cm²)
Pulses (N):
0 to 500 shots studied
Optics:
9×9 lens array for uniform spot; 2 biconvex lenses
CA Meter:
OCA20 (DataPhysics); 3 µL drops; 5 measurements/site
Characterisation:
AFM (PicoScan 2500), SEM (FEI Quanta 200), XPS (AXIS Ultra)
Fig. 8 – Static CA vs. laser shots at 5 fluences (Liu et al., 2010)
Fig. 9 – AFM (a,b) & SEM (c–e) images of PVDF surfaces
Key Findings:
Maximum CA = 170° at 400 mJ/cm², 20 pulses (from 53°). Superhydrophobicity achieved in seconds (< 1 minute!). At ≥ 300 mJ/cm², surface damage occurs but CA remains > 150°. At lower fluences (100–200 mJ/cm²), ~200 pulses needed — 10× longer process.

## Slide 15
Exp. 3 — PVDF: XPS Analysis & Hydrophobicity Mechanism
Fig. 10 – XPS spectra: (a) survey before/after irradiation, (b) C 1s deconvolution after irradiation, (c) F 1s spectra (Liu et al., 2010)
Before Irradiation
PVDF dominated by CH₂ (286.42 eV) and CF₂ (290.84 eV) bonds. C 1s: 46%. F 1s: 44%. Contact angle: 53°.
After KrF Irradiation
New bonds appear: C–CF₂ (21%), C–F (15%), C–F₂ (12%). F 1s shows C–CF₂ and C–F peaks. These lower surface energy → superhydrophobicity.
Mechanism
KrF laser thermal energy causes photochemical cleavage of C–H and C–F bonds → C–CF₂ and C–F form → regular wall-like 3D structure + reduced surface energy → CA up to 170°.

## Slide 16
EXPERIMENT 4
Superhydrophobic Textures on
Stainless Steel 316 (SS316)
Generation of Super-hydrophobic Textures Using a Nanosecond Pulsed Laser Machine
— Dongre, Rane, Raut et al. (AIP Conf. Proc. 2023)

## Slide 17
Exp. 4 — SS316: Experimental Setup & Microscopic Results
Experimental Parameters
Material: SS316 plates, 30×30 mm, 1 mm thick
Laser: NUQA-1064-NA-0030-YZ, 30W max, 100±20 ns pulse
Power: 30%, 40%, 50% (= 9W, 12W, 15W)
Scan Speed: 200, 250, 300 mm/s
Frequency: 70, 80, 90 kHz (Taguchi DOE)
Pattern: 10×10 mm square, horizontal hatches, 150 µm spacing, 66 hatches
Microscope: Rapid I-vision for hatch width/depth
Fig. 1 — Nanosecond Pulse LASER machine (NUQA-1064-NA)
Fig. 11 — Rapid I-vision microscopic images of LASER textured SS316 surfaces (Dongre et al., 2023)

## Slide 18
Exp. 4 — SS316: Results — Width, Depth & Material Removal Rate
Fig. 12 — Hatch Width vs. Parameters
Fig. 13 — Hatch Depth vs. Parameters
Fig. 14 — MRR vs. Parameters
Key Findings
Width Trend
Decreases at 40% power then rises at 50%. Power has the sharpest influence on kerf width.
Depth Trend
Increases with power; decreases with scan speed. Frequency stabilizes at 80–90 kHz.
MRR Trend
Dip then rise with all three parameters. Units: mm³/s. Max at 50% power, 200 mm/s.
Optimal Params
9–12W, 70–80 kHz, 250–300 mm/s → CA > 150° (lit. ref.)

## Slide 19
Comparative Summary of All Three Experiments
Parameter | Exp. 1 — Si (001) | Exp. 2 — Polycarbonate | Exp. 3 — PVDF
Laser Used | ArF (193 nm) KrF for comparison | KrF (248 nm) 25 ns pulses | KrF (248 nm) 30 ns pulses
Sample Material | Si (001) wafer (n-type, P-doped) | Polycarbonate film 1 mm thick | PVDF film 0.5 mm thick
Irradiation Medium | Methanol solution (CH₃OH) | Ambient air | Ambient air
Fluence / Pulses | 65 mJ/cm², 800 pulses | 20–100 mJ/cm² 2000 pulses | 100–400 mJ/cm² 20–500 pulses
Max CA Achieved | 103° (hydrophobic) | > 150° (superhydrophobic) at > 80 mJ/cm² | 170° (superhydrophobic) at 400 mJ/cm², 20 pulses
Mechanism | Chemical: Si–OCH₃ bond formation | Physical: micro/nano structures + carbonization | Both: C–CF₂/C–F bonds + wall-like structures
Characterisation | AFM, XPS, CA | SEM, CA, E.coli test | AFM, SEM, XPS, CA
Key Application | Microfluidics, lab-on-chip | Medical implants, antibacterial surfaces | Electronics, piezo- electric devices

## Slide 20
Conclusions
01
Excimer laser (ArF/KrF) irradiation is a powerful single-step technique to generate hydrophobicity on diverse materials — Si, PC, and PVDF.
02
Two distinct mechanisms operate: chemical modification (Si–OCH₃ on Si; C–CF₂/C–F on PVDF) and physical structuring (ablation-induced micro/nano topography on PC).
03
Superhydrophobicity (θ > 150°) is achievable on polycarbonate and PVDF via appropriate laser fluence, enabling self-cleaning and antibacterial functionality.
04
On Si, hydrophobicity (θ = 103°) is purely chemical with no detectable surface morphology change — confirmed by AFM (R_RMS unchanged at ~0.37 nm).
05
Laser parameters (fluence, pulse number, wavelength) are critical: KrF cannot photodissociate methanol; above-threshold fluence creates micro-structures; below-threshold causes hydrophilicity on PC.
06
These findings have broad applications in biomedical implants, microfluidics, antibacterial surfaces, and semiconductor fabrication.