## Slide 1
Hydrophobicity Generation
on Oxide Substrates
A Focused Literature Review on SrTiO₃, MgO, and Al₂O₃
SrTiO₃
MgO
Al₂O₃

## Slide 2
SrTiO₃ (Strontium Titanate) — What is Reported in Literature
Perovskite oxide used as substrate for thin film deposition. Intrinsically hydrophilic due to high surface energy.
Ti:Sapphire Laser + Sol-Gel → STO Nanoparticle Synthesis
Energy: 20.3 kJ/m² and 240 mJ/cm² · Focus: crystallisation improvement, NOT wettability
Laser pulses improve crystallinity of STO nanoparticles. Hydrophobicity not addressed.
DOI: https://doi.org/10.1016/j.jmst.2020.07.024
Picosecond Laser Grooving → Super-Hydrophilicity on STO
Material: Single-crystal SrTiO₃ · Method: Picosecond laser grooving
Result: WCA → ~0° (super-hydrophilic). Wettability goes in the OPPOSITE direction.
DOI: semanticscholar.org/paper/58f239f375d79c876c39adc19faab83b124ab1ce
OTS Self-Assembled Monolayer on SrTiO₃ → Hydrophobic Film
Method: Octadecyltrichlorosilane (OTS) SAM, dip-coating · CA > 110° achieved
NOT laser-based — chemical self-assembly. OTS film ~2.4 nm thick.
DOI: 10.1016/S0040-6090(98)00625-7
Femtosecond Laser LIPSS on SrTiO₃ — Structural Study Only
fs laser irradiation on single-crystalline STO — LIPSS nanostructure formation studied
2D→1D LIPSS transition with pulse number. Wettability NOT reported.
DOI: https://doi.org/10.1002/adom.202502761

## Slide 3
SrTiO₃ — Summary of Wettability Literature
Intrinsic Nature
SrTiO₃ is naturally superhydrophilic. DFT and STM studies confirm strong water–surface interaction on (001) and (110) facets.
Laser Work: Synthesis-Focused
Ti:Sapphire and picosecond laser studies target crystallisation improvement and nanoparticle synthesis — not hydrophobicity.
Laser Grooving → Hydrophilicity
Picosecond laser grooving on single-crystal STO enhances super-hydrophilicity (WCA → 0°) — opposite of what is needed.
Chemical SAM Route (OTS) — Hydrophobic
OTS monolayer on STO achieves CA > 110°. However, this is dip-coating, not laser-based. (Thin Solid Films, 1998)
LIPSS Study — Structure Only
fs laser LIPSS on SrTiO₃ studied for structural/electrodynamic properties only — wettability not reported.
⚠ Laser-induced hydrophobicity on SrTiO₃ has NOT been reported. Existing laser work yields hydrophilicity.

## Slide 4
Al₂O₃ (Alumina) — What is Reported in Literature
Hard ceramic oxide. Initial WCA ~115°. Extensive laser hydrophobicity literature exists on this material.
Picosecond UV Laser (6.7 ps) → Superhydrophobic Al₂O₃ — Single-Step
Energy: 2.82 J/cm² · Micropillars and microholes (100–1200 pulses/unit area) · No chemical post-treatment
Result: Superhydrophobic surface. Geometry is key driver, not chemical composition.
DOI: 10.1021/la5033527 [ACS Langmuir, 2014]
Nanosecond Fiber Laser (1064 nm, 50 ns) → Hydrophobicity + Improved Tribology
Ytterbium fiber laser on Al₂O₃ · Varying fluence and hatch parameters . %0.93 J/cm2
Result: Significantly improved hydrophobicity and friction stability. XPS confirmed wettability mechanism.
DOI: 10.1364/AO.423564 [Applied Optics, 2021]
CO₂ Laser + N₂ Gas Assist → Hydrophobicity via AlN/AlON Compounds
CO₂ (2 kW), N₂+O₂ assist at 600 kPa · Alumina tiles 4 mm thick
Micro/nano pillars + AlN/AlON compounds increase hardness ~50% and enhance hydrophobicity.
DOI: https://doi.org/10.1016/j.apsusc.2013.09.040
Femtosecond Laser → Super-Hydrophilic Al₂O₃ (Persistent, >40 days)
Triangular groove patterns, depths 3.2–17.1 µm · Deeper grooves: θ < 5° for >40 days
Thermal anneal (120°C) gives transient CA ~148.9°, decays to ~90° within 6 weeks.
DOI: 10.3390/mi17010029 [Micromachines, 2026]

## Slide 5
Al₂O₃ — Summary of Wettability Literature
Superhydrophobicity: Confirmed via Picosecond Laser (Single-Step)
UV ps laser (6.7 ps) — micropillars and microholes produce superhydrophobic surfaces in one step. Geometry dominates over chemistry.
Hydrophobicity: Confirmed via Nanosecond Fiber Laser
Ytterbium fiber laser (1064 nm, 50 ns) texturing improves hydrophobicity and tribological performance of Al₂O₃ ceramic.
Hydrophobicity with Nitrogen Gas Assist: CO₂ Laser
CO₂ laser + N₂ gas creates AlN/AlON compounds alongside micro/nano pillars — texture and chemistry both contribute.
Femtosecond Laser → Hydrophilicity (Opposite Direction)
Deeper grooves give persistent superhydrophilicity (θ < 5°). Thermal annealing gives transient hydrophobicity (~148.9°) that decays to ~90° within 6 weeks.
Silanization After Laser Texturing → Superhydrophobicity
Al₂O₃ texturing + fluorosilane coating reliably gives superhydrophobic surfaces. Multiple sources confirm this combined approach.
⚠ Al₂O₃ is extensively studied for laser hydrophobicity — NOT a novel research target.

## Slide 6
MgO (Magnesium Oxide) — What is Reported in Literature
Alkaline metal oxide. Intrinsically hydrophilic in bulk; MgO crystal surfaces show unusual molecular-level hydrophobic character.
Nano-Magnesia in Cotton Fabric → Superhydrophobicity (Chemical, Not Laser)
Material: Cotton fabric + MgO nanoparticles · Method: Chemical surface modification only
Result: Nano-magnesia gives superhydrophobicity to fabric. No laser involved.
DOI: https://doi.org/10.1080/00405000.2023.2258047 [Textile Research Journal, 2023]
Nanosecond Laser on Mg Alloy → MgO Nanoparticle-Decorated Superhydrophobic Surface
Material: Mg alloy (MA8) · Laser → MgO nanoparticles on surface · Then: fluorosilane CVD
Hierarchical roughness + MgO nanoparticles; wettability: superhydrophilic → superhydrophobic.
DOI: https://doi.org/10.3390/ma14185454 [Materials, 2021]
Nanosecond Laser on Mg → MgO Layer Morphology (Corrosion Study)
Pure Mg · ns laser in N₂ and CO₂ atmospheres · Focus: degradation behaviour
Higher roughness MgO gives better corrosion resistance. CA studied as secondary parameter.
DOI: https://doi.org/10.1016/j.vacuum.2023.111913 [Vacuum, 2023]
Molecular Dynamics + vSFG: MgO Crystal Shows Molecular Hydrophobicity
MgO(100) and MgO(111) · vSFG spectroscopy + contact angle · J. Phys. Chem. C, 2021
DOI: https://pubs.acs.org/doi/10.1021/acs.jpcc.1c06486?ref=pdf

## Slide 7
MgO — Summary of Wettability Literature
No Laser-Induced Hydrophobicity on MgO Bulk Crystal Reported
No published work found on laser-based hydrophobicity generation on MgO as primary substrate. Existing work uses MgO as a by-product of Mg alloy processing or as a nanoparticle modifier.
Nano-MgO as Surface Modifier (Chemical Route)
Nano-magnesia nanoparticles give hydrophobicity to cotton via chemical modification — NOT laser texturing of MgO itself. (Textile Research Journal, 2023)
MgO Forms as Laser By-Product on Mg Alloys
Laser-processed Mg alloys produce MgO nanoparticles on the surface. These can be rendered hydrophobic via fluorosilane CVD. Substrate is Mg alloy, not MgO crystal.
Intrinsic MgO Crystal: Molecular-Level Hydrophobicity
vSFG spectroscopy shows MgO(100) and MgO(111) display non-H-bonded OH modes — unusual molecular-scale hydrophobicity distinct from other metal oxides.
Chemical Modification (hfacH) Confirms Tuneable Surface Energy
MgO modified with hexafluoroacetylacetone (hfacH) shows shifts in hydrophobicity, confirming the surface energy is tunable — but laser work is absent.
★ Laser-induced hydrophobicity on MgO bulk crystal has NOT been reported — a potential novel research direction.

## Slide 8
Comparative Summary: SrTiO₃ vs Al₂O₃ vs MgO
Aspect
SrTiO₃
Al₂O₃
MgO
Intrinsic Wettability
Superhydrophilic
(high surface energy)
Hydrophobic initially
(WCA ~115°)
Hydrophilic (bulk)
Molecular hydrophobicity
(crystal surfaces)
Laser Hydrophobicity
Work
None found — laser
gives hydrophilicity
or synthesis-focused
Extensively reported:
ps, ns, CO₂ lasers
all give hydrophobicity
None found on bulk
MgO crystal/substrate
Chemical Route
Hydrophobicity
OTS SAM on STO
CA > 110°
(dip-coating)
Laser texture +
silanization →
superhydrophobic
Nano-MgO in fabric;
hfacH modification
on MgO surface
Key Gap /
Novel Opportunity
Laser → hydrophilic
only. Not novel
for hydrophobicity
Well-studied.
NOT a novel
target
Laser hydrophobicity
on MgO bulk crystal
NOT reported ★
★ MgO is the most promising novel target: no laser hydrophobicity work exists, and its crystal surface shows unusual intrinsic molecular hydrophobicity.

## Slide 9
Recommendation: Pursue MgO
1
No Laser Hydrophobicity Work on MgO Bulk Crystal Found
Despite thorough searching, no published paper on laser-induced hydrophobicity on MgO substrate was identified. This is a genuinely novel research direction.
2
Intrinsic Molecular Hydrophobicity at Crystal Level
MgO(100) and MgO(111) display non-H-bonded OH vibrations (~3700 cm⁻¹) — unusual molecular hydrophobicity unlike most metal oxides. A strong scientific starting point.
3
Chemical Routes Confirm MgO Surface Energy is Tunable
Nano-magnesia fabric modification and hfacH chemical treatment both show MgO surface energy can be altered toward hydrophobicity. No one has used laser texturing to achieve this.
4
SrTiO₃ and Al₂O₃ Already Explored or Ruled Out
Al₂O₃ has extensive ps/ns/CO₂ laser hydrophobicity literature — not novel. SrTiO₃ laser work gives hydrophilicity. MgO remains unexplored as a laser hydrophobicity target.